MSU – Materials Testing and Characterization Equipment

Agricultural & Biological Engineering (Contact: Steve Elder)

    - Instron Model 1011, screw driven load frame - 1000 lb. 			Additional load cells – 22, 220, 2200 kg.

    - MTS Bionix 858, Servo-hydraulic load frame - 5000 lb.

Capacity Load calibration ranges – 1100, 11000 kg

Displacement calibration ranges – 12.7, 127 mm

Cyclic testing up to 5 Hz

    - MicroStar AO Inverted Microscope

    - Cell Culture Facilities:

Class II A/B3 Biological Safety Cabinet

    - Fisher Scientific Carbon Dioxide Incubator

      - Precision Model 183 Water Bath

    - VWR AS10 Autoclave and Centrifuge

    - EG&G Instruments  Model 6310 – with data collection system 			Electrochemical Impedance Analyzer  AC & DC current corrosion

    - Rockwell Hardness Testing – A, B, & C scales

# Aerospace Engineering

Raspet / composites:   (contact:  Matt Fox)

- 5-axis Gantry machine

- 5-axis Arboga milling/polishing machine

- Autoclaves:

4 ft. dia. x 16 ft., 100 psi, 350º F

10 ft. dia. x 55 ft., 300 psi, 800º F

2 ft. dia. x 4 ft, 300 psi, 800º F

- 3 ovens for 350º F vacuum bag fabrication (6, 14, & 40 ft.)

Fatigue and fracture mechanics laboratory: (contact: Jim Newman, Jr.)

- 25 kip  Satec  - with data collection system

servo-hydraulic test machine

fatigue loading up to 10 Hz

Load Cells - 5,000 and 20,000 lb

- 4 – 6 kip Instrons – with data collection system servo-hydraulic test machines fatigue loading up to 20 Hz Load Cells – 225, 1, 100, 5,600 lb and 4 – FTA Automatic crack-monitoring systems

## CAVS (Contact:  Steve Horstemeyer)
I)	Mechanical characterization

## 1)	350KN Instron Servohydraulic tension/torsion machine

## 2)  	100KN MTS servohydraulic machine

## Dynamical extensometer with adjustable gage lengths

## 3)   50KN Instron Electromechanical machine with climatic chamber (-60F ~ 370F)

## 4)   100KN Instron Electromechanical machine with climatic chamber (-60F ~ 370F)

## 5)   Lavision 3D optical strain measurement system with a Questar telescope

6)   Fullam EM SEM Tensile stage and fatigue stage (for in-situ SEM testing)

## 7)   Hopkinson bars:  Compression, Tension, Torsion

## 8)   Instron Servohydraulic Erector Set with 4 servohydraulic actuator ( 25, 50, 100, 250 KN) for structural testing

## 9)	Hysitron Triboindenter/ nanoindentation / scratch modes

10) LECO LM 300 Micro hardness Tester

11) LECO LR Rockwell Hardness Tester

12) Corrosion tank

## II)	Microstructural Characterization and Quantification 
		1)	Phoenix X-ray Computed Tomography (2D and 3D);
					Dual tube: Microfocus 225KV and Nanofocus 160KV
					Resolution up to 800nm 
		2)	ZEISS SUPRA 40 Field Emission Gun Scanning Electron Microscope 					(FEG-SEM) with EDX and EBSD

## 3) 	Zeiss Axiovert 200 MAT Inverted microscope

## (5 Objectives, Magnification up to 2500X) 
		3)	Talysurf

## Non-contact measurement

## Contact measurement (Higher resolution)

## "3D" reconstruction of free surfaces

## III)		Processes:

## Rand Castle RCPR-0625 Extruder with 5 Zone control panel and standard die

- Arburg Injection Molding Machine

## High temperature Furnaces (1100º C)

## Microbalance

## Automatic polishers for polishing mechanical samples

## Manual polishers for polishing mechanical samples

## Oven, vibrometer, fume hood, various etching solutions

## Planned Nickel plating

## Polishers for round and flat fatigue mechanical samples

## Dilatometer, 1650 C, dual pushrod in hydrogen, nitrogen, argon, or vacuum

- Flaming Tensile Tester (FTT): in situ strength measure, 850º C

- Accu Pyc 1330 Micromerities: a helium pycnometer

- TSI Amherst Aerosizer: particle size analysis by time of flight

- Carver Molding Press

- Double Cone Blender

- Hall Flowmeter

- HASS CNC milling and lathe machines

- Rheology Testers

  - Setaram Instrumentation TGA/DTA, and DSC-131

  - TA Instruments DMA Q800

  - Thermo Electron Corp. FTIR

Chemistry

Contact: Bill Henry

- Bruker SMART 1000 Single Crystal Diffractometer

- Perkin Elmer DSC7

- Perkin Elmer  TGA 7

Contact:  David Wipf

- AFM and STM  (Thermomicroscope)

- Scanning Electrochemical Microscope (SECM)

- Frequency Response Analyzer and Electrochemical Interface (Solartron)

- Electrochemical Workstation (BAS)

- Rotating Disk Electrode (Pine)

## Chemical Engineering

## Contact:  Keisha Walters

- Auger, XPS, and RAMAN spectroscopy

- MDSC – TA Instruments Q2000 Modulated Differential Scanning Calorimeter with Autosampler and Mass Flow Control, and an RCS90 Refrigerated Cooling System (temperature range from -90 °C to 550 °C).

- STA – TA Instruments Q600 SDT Simultaneous DSC-TGA

Contact:  Hossein Toghiani

- Zwick – 1000 lb screw driven test machine

- Izod Impact Testing

Civil Engineering  (contact:  Tom White or Chris Saucier)

- Tinius Olsen 300,000 lb screw driven load frame with:

10 ft square loading bed

17 ft throat opening

- Baldwin 200,000 lb hydraulic load frame with:

10 lb incremental loading

6 ft throat opening

- 4 each 250kip hydraulic load frames and controllers

- Planed addition of a 1000 kip load frame.

- 8000 lb overhead hoist extends 30 ft. outside building

- facility has large doors (6 ft. x 18 ft.)

Electrical & Computer Engineering (contact:  Yaroslav Koshka)

- Silicon carbide chemical vapor deposition (CVD) system

- DC and RF sputtering tools

- 6 tube 3-zone diffusion furnaces

- Photolithographic equipment

- Semiconductor electrical characterization suite

I2AT (Contact:  Giselle Thibaudeau)

    - Transmission Electron Microscope – JEOL 100CX II
		Accelerating voltage: 100 kV
		Magnfiication range: 100X to 450,000X
		Resolution 4.0A (point-to-point), 2.0A (lattice)

    - Scannning Electron Microscopes
	     JEOL JSM-6500F Field Emission SEM
		Accelerating voltage: 0.5 to 30 kV
		Magnification range: 10X to 500,000X
		Resolution: 15A @ 15kV
			with attached Oxford Instruments X-EDS and WDS 				spectrometers and EBSD detector

    - Carl Zeiss EVO50 SEM with LaB6 emitter, Bruker X-EDX spectrometer

- Accelerating voltage: 0.5 to 40 kV
			Magnification range: 10X to 300,000X
			Resolution: 25A
			Cathodoluminescence detector

- Hitachi table-top scanning electron microscope (outreach activities)

- Atomic Force Microscope Suite

Includes:Biological Sample AFM (Bio-AFM),

Large Sample, General Purpose AFM (LSGP-AFM),

Portable, Easy-Use AFM for Education and outreach activities.

Electrochemical STM attachment for Bio-AFM or LSGP-AFM.

- GE 3 Tesla Magnetic Resonance Imaging (3T MRI)

- Biological specimen preparation equipment

- Materials science specimen preparation equipment for TEM

    - Confocal laser scanning microscope
		Axiovert 200 M Inverted Research microscope
		3 confocal detection channels
		Laser lines: 405, 458, 477, 488, 514, 543, 594, 633

    - X-Ray diffraction systems
		Rigaku Ultima III powder diffractometer (Bragg-Bentano 				Geometry) with Cu-kA x-rays (0.154 nm wavelength); will scan 			from 2theta/theta - 3 to 154 degrees

		Rigaku SmartLab diffractometer

    - rocking curve,

    - texture,

    - pole figures,

    - residual stress,

    - small angle scattering,

    - in-plane diffraction,

    - hot (900 deg C) stage

Forest Products (Contact:  Rubin Shmulsky)

- X-ray scanner: 24 inches wide, 6 inches tall.

- 600 kN UTM, computer controlled,  25' long base

- Hot press, 30" x 30" platens, 400 F

- Cold Presses, 20' length

- Varying load limits on electo-mechanical load frames.

ICET (contact: Ron Palmer)

## Mechanical Engineering (Contact:  Judy Schneider)

- Image Analysis System and sample preparation facilities

- Small melting and heat-treatment facilities

- Rockwell Hardness Testing – B, & C scales

- Instron 10 kip test machine with data acquisition

Electro-mechanical system

Tension grips and compression platens